# Supporting Information

# Evaluating of the methylene blue removal on plasma activated palygorskites

Heldeney Rodrigues de Sousaa, Lucinaldo dos Santos Silvab, Patrícia Alves de Abreu e Sousaa, Rômulo Ribeiro Magalhães de Sousac, Maria Gardênnia Fonsecad, Josy Anteveli Osajimaa, Edson Cavalcanti da Silva Filhoa,*

aInterdisciplinary Laboratory for Advanced Materials – LIMAV, UFPI, 64049-550, Teresina, PI, Brazil,

bFederal Institute of Maranhão, Açailândia Campus, IFMA, 65930-000, Maranhão, MA, Brazil,

cDepartment of Mechanics, Federal Institute of Piauí, IFPI, 64000-040, Teresina, PI, Brazil and Department of Mechanical Engineering, Federal University of Piauí, UFPI, 64049-550, Teresina, PI, Brazil

dResearch and Extension Center - Fuel and Materials Laboratory (NPE – LACOM), Federal University of Paraíba, UFPB, 58051-900, João Pessoa, PB, Brazil

*Corresponding author: Tel/Fax: +55-86-32215710. E-mail: edsonfilho@ufpi.edu.br

Fig. S1. Scheme of experimental setup, Ar – argon, H2 – hydrogen and N2 – nitrogen bottles,  M1, M2 and M3 – mass flow controller, PV – pump vacuum,  AE – air entrance, T- thermostate and VC – vacuum camera.

Fig. S2. X-ray dispersive energy spectra for the pristine and plasma activated palygorskites.

PAL-6H

PAL-4H

PAL-2H

PAL-N

Fig. S3. Effect of adsorbent mass (m) on MB adsorption for the pristine and plasma activated palygorskites.

Fig. S4. Effect of pH on MB adsorption by pristine and plasma activated palygorskites

Fig. S5. (a) Distribution of MB species at different pHs and (b) proposal for MB adsorption on the plasma activated palygorskites.

| (1) (2) | (3) (4) |
| --- | --- |

(a)

(b)

Fig. S6. Linear fitting of the influence of time (t) on adsorption to the pseudo-first-order model for the methylene blue adsorption by PAL-N, PAL-2H, PAL-4H and PAL-6H.

PAL-4H

Fig. S7 Linear fitting of the influence of time (t) on adsorption to the pseudo-second-order model for the methylene blue adsorption by PAL-N, PAL-2H, PAL-4H and PAL-6H.

Fig. S8. Linear fitting of the influence of time (t) on adsorption to intraparticle diffusion model for the methylene blue adsorption by PAL-N, PAL-2H, PAL-4H and PAL-6H.

Fig. S9. Linear fitting of the adsorption data to Langmuir model for the methylene blue adsorption by PAL-N, PAL-2H, PAL-4H and PAL-6H.

Fig. S10. Linear fitting of the adsorption data to Freundlich model for the methylene blue adsorption by PAL-N, PAL-2H, PAL-4H and PAL-6H.